Leaching of Zinc Sulfide in the presence of manganese dioxide and ammonium persulphate as oxidative agents

Ehsan Ebrahimi ¹, Mohammadreza Shahbazi ², Gholamreza Karimi ³

¹ Department of mining and mineral Engineering Imam Khomeini International University, Qazvin, Iran, ebrahimieng1@gmail.com

² Department of mining and mineral Engineering University of Tehran, Tehran, Iran, Mrshahbazi98@ut.ac.ir

³ Department of mining and mineral Engineering Imam Khomeini International University, Qazvin, Iran, gh.karimi@eng.ikiu.ac.ir

Abstract

Recovery of zinc from sulfide mineral Mehdi Abad Yazd ore mine, by direct oxidative leaching in the presence of manganese dioxide and ammonium persulphate as oxidative agents was studied and showed that ammonium persulphate was improved oxidant than other persulphate salts. So the purpose of this paper is study on effects of kinetic parameters such as particle size, temperature, acid concentration, effect of ferric and ferrous on zinc dissolution, and describe kinetic model by shrinking core model (SCM), through direct oxidative leaching in presence of sulfuric acid media, Manganese dioxide (MnO2) and Ammonium persulphate individually, as oxidative agents. Based on results The optimum leaching conditions were determined to be: particle size +75µm_+45µm, acid concentration of 5% (v/v) and in presence of manganese dioxide 20% (w/v), and it was investigated that there is a significant impact on the recovery temperature increase especially in the temperature of    85 ° C maximum amount to their recovery. The kinetic data was analyzed by SCM. The new SCM variant fits the kinetic data more appropriately and finally the activation energy was calculated to be Ea=21.78 kJ/mol.

KEYWORDS: LEACHING, OXIDATIVE AGENTS, KINETIC MODEL, SULFIDE MINERAL

- Introduction

Amongst the non-ferrous metals, zinc is one of the most used metals after aluminum and copper. Zinc is an important metal required for many applications, from metal products to chemical, paint, and agriculture industries. It is mainly recovered from sphalerite (ZnS), which is found in metamorphic, igneous, and sedimentary rocks in many parts of the world [1, 2]. One of the most important subject in zinc industry is finding suitable techniques that obtains zinc from zinc sulfide or silicates minerals, because of reducing zinc oxide minerals resources in Iran.

Leaching is an essential part in the hydrometallurgy [3].Also, there are several techniques to extract zinc from sulfide minerals such as; the roasting−leaching−electrowinning (RLE) process, that is the main way to product zinc and responsible for more than 85% of zinc production in the world [4]. Producing SO2 in the (RLE) process cause’s air pollution, which is a big challenge to the RLE process [5]. In the 1980s, another the new process of zinc pressure leach (ZPL) was developed, which zinc sulphide concentrate is directly leached and the sulphidic sulfur is oxidized to elemental form rather than to SO2, so that the pollution of SO2 is completely avoided. Although the ZPL process makes the zinc industries more competitive, it needs high-cost autoclave and its application is limited [6].

In the 1990s, the atmospheric direct leaching (ADL) process of zinc sulphide concentrate was developed [7]. Actually, the ADL process is operated under oxygen-rich conditions, which is similar to low-temperature pressure leaching know-how [8, 9]. The ADL process has been practiced at an industrial scale [10, 11]. In 2008, Zhuzhou Smelter Group, the leading Chinese zinc producer, integrated the ADL process with the existing production plant to increase zinc production capacity by 100000 t/a [12]. The ADL process is still in development to promote the leaching rate of zinc sulphide concentrate. The acidic dissolution and the subsequent oxidation of H2S are assumed as main reactions during the ADL process of sphalerite [13].

Direct oxidative leaching is another zinc extraction method, this process has lower costs than other zinc extraction methods. Using direct oxidative leaching prevents release the SO2 gas therefore, it is better compatible with the environment than other methods [14]. Researchers have used different materials as oxidative agents during the direct oxidative leaching. Teresa et al, used hydrogen peroxide as an oxidative agent and showed that the addition of oxidative agents helps to increase the leaching rate [15].

In present investigation, zinc extraction experiments from a sphalerite concentrate with precipitation of iron using the direct leaching process at lab-scale was conducted. A parametric study was carried out also using the results obtained by other researchers under deferent leaching conditions to evaluate the factors influencing the leaching process of zinc concentrates. Effect of different parameters on direct oxidative leaching of sphalerite was studied and kinetic study was also conducted to determine the model and the rate-determining step from the experimental results and other data reported in the literature.

# MATERIAL AND METHODS

## Preparation sample and chemical materials

The ore sample was prepared from Mahdi Abad mine, located in Yazd, Iran. The X-ray diffraction (XRD) analysis of sample shown that sphalerite (ZnS) is the main mineral of the sample, moreover the XRD analysis showed that the sample contains other minerals such as smithsonite, hemimorphite, chalcophanite, zincite and some other minerals. Due to the effectiveness of each mineral during leaching process, every different chemical reaction separately investigated and influence of theses minerals on zinc dissolution was considered. The atomic absorption spectroscopy (AAS) analysis, showed amount of metals contained in the sphalerite sample; 6.90% Zn, 23% Fe, 2.24% Pb, 3.71%Mn, and 1.87% Cu.

The ore sample was ground that it crushed and sieved in the -150µm to +45 µm sizes, But in experiments the -105µm_ +75 µm was used, this ground sample was weighted and used for leaching tests.

## Experimental methods

The direct oxidative leaching of sulphide samples are taken place in beaker at 400 mL of water under heater and electro mixer with 490 rpm, (rotation per minute), details of the experiments was reported in this paper: the leaching tests are carried out in such situations as follows: the sulfuric acid (H2SO4) was used, The pH range of leaching solutions was controlled between 2.5 – 3.5, and leaching time was 3 hour (180 minutes), at 65ºC temperature. In this study, sulphuric acid and Manganese dioxide (MnO2) and Ammonium persulphate were used individually, as oxidative agents. The sulfuric acid concentration of 5% (v/v) and the oxidative agent's concentration of 20% (w/v), were used in experiments.

Base on this studding kinetic reaction of sphalerite in direct oxidative leaching and effects such as; acid concentration, particle size of ore sample, and amount of oxidative agents, different temperatures, and type of oxidative agents that used in leaching process was surveyed.

First effect of acid concentration on the dissolution was checked, then performance of each oxidative agent examined also, the best amount of acid concentration and oxidative agent type, was determined. Then effect of other kinetic parameters on zinc dissolution was studied. Finally appropriate kinetic model conditions were introduced and chemical process analyzed according to the shrinking core model (SCM). These conditions describe original leaching process whereas effect of each kinetic parameter was measured alone. In the each step of the reaction progress, the zinc recovery reaction during each process was calculated by using AAS analysis. Finally after each experiment the materials deposited after leaching process were filtered with filter paper, and weighed, then filter materials for drying were placed in the oven for 24 hours and after that dried material weight were measured and amount of zinc in the products was computed by AAS analysis to calculate the recovery.

Figure 1: The X-ray diffraction (XRD) analysis of sample

# RESULTS AND DISCUSSION

According to the results of XRD analysis, it is clear that the main zinc mineral is sphalerite, and there are other zince bearing minerals, which included Smithsonite, Hemimorphite, Franklinite, Chalcophanite, Wurtzite, and Zincite. Based on the results of AAS analysis, it is known that the amount of ferrous ions in this solution is significant, the reaction of sphalerite in sulfuric acid in presence of manganese dioxide, followed by Eq.1:

[Equation 1]:

ZnS s+ 2 H2SO4 aq + MnO2s→ ZnSO4aq+  MnSO4aq+2H2O aq+ S s

Due to the existence of ferrous ions in solution, the reaction between manganese dioxide and ferrous ions occur followed by Eq. (2) and reaction between the ZnS with high Fe+3 concentration follows Eq. (3)

[Equation 2]:

2 Fe+2aq+ MnO2s+ 4 H+aq→ 2 Fe +3aq+ Mn+2 aq+ 2 H2Oaq

[Equation 3]:

2 Fe +3aq+  ZnSs+ 2H+aq→2 Fe+2aq+  Zn+2 aq+2H+aq +Ss

Jan et al Indicated, that the minerals in the solution was oxidized through the ferric ions [16, 17]. Also, re-oxidize the ferrous ions to the ferric form was accomplished by the oxygen in the reaction. In present work, according to Eq (2), this option was done by manganese dioxide. In fact, the main role of manganese dioxide or other oxidative agents is re-oxidize the ferrous ions to the ferric ions that role in the dissolution of sphalerite du to Eq (3). This process also has been recognized by other researchers Verbaan, B., Crundwell, F.K et al [18].

In this work, the usage of ammonium persulphate as oxidants, investigated that the chemical processes of this reaction is similar to the previous mode reaction and oxidative agents has effect on the re-oxidizing the ferrous ions to the ferric ions.Eq. (4-9):

[Equation 4]:

2FeSO4aq+NH42 S2O8S→ Fe2SO43 aq+NH42 SO4aq

Reduction reaction: 
[Equation 5]:                             8O-148+2e-→8O-

Oxidation reaction:

[Equation 6]:                              2 Fe+2 -2e- → 2 Fe +3

[Equation 7]:

ZnS s+Fe2SO43 aq → ZnSO4aq+2FeSO4+S(s)

Oxidation reaction:

[Equation 8]:                                    S-2-2e-→S0

Reduction reaction: [Equation 9]:         2 Fe+3+2e- → 2 Fe +2

Therefore, based on the above reactions, it is assumed that in both cases oxidative agents cause the ferrous ions re-oxidize to the ferric ions, then the ferric ions performances as dissolution agent to solution zinc during reactions.

Effect of acid concentration

According to “Figure.2”, experiments show that zinc recovery increases with additional of acid concentration. This recovery reaches to a certain amounts that it's visible. This amount of acid concentration is around 5%, while increasing the amount of acid to a percentage more than 5%, recovery is reduced.  Similar results can be found in the investigation of F.K. CRUNDWELL and B. VERBAAN et al [19] .However it was observed that the PH grew during progress of reaction; PH adjustment reactions play an important role in the development of zinc dissolution so this parameter also is impressive by changing the amount of acid concentration.

Figure.2: Effect of acid concentration H2SO4 (%), on Zinc recovery. particle size -105µm_ +75 µm Temperature 338 K, oxidant 20% (w/v) MnO2.

Effect of different oxidative agents

In this part, type of oxidative and their performance on leaching was studied. The reaction was done by two types of oxidative agents individually, while remains of reaction conditions became constant. Effect of the type of oxidative agents on zinc recovery has been shown in Figure 3.

Results of two experiments indicated that; manganese dioxide shows better performance than ammonium persulphate during leaching. According to “figure 3”, although in the first 25 minutes of reaction, ammonium persulphate has a better performance than manganese dioxide on the zinc recovery after 25 minutes of reaction manganese dioxide has better performance on the zinc recovery.

Figure 3: Effect of different oxidative agents on Zinc recovery. Particle size -105µm_ +75 µm Temperature 338 K, H2SO4 5% (v/v).

Effect of temperature

According to the results and “Figure 4” that was done under these conditions: particle size +75µm_+45µm, acid concentration of 5% (v/v) and in presence of manganese dioxide 20% (w/v), it is clear that increasing temperature has a significant impact on the recovery. Especially in the temperature of    85 ° C maximum amount recovery was obtained. Of course According to Arrhenius equation, effects of temperature on the chemical rate remain constant.

Figure4: Effect of temperature, particle size -75µm_+45µm, acid concentration of 5% (v/v) and manganese dioxide 20% (w/v) as oxidative agent.

The stage of control reaction

in the present reaction contained sulphide minerals, when the dissolution of the product are penetrating into the solution from surface, the sulfur layer trying to stay on the surface . As a result the availability of reactants to the surface of sphalerite prevented by this sulfur layer.

In solid phase, morphology has extremely effect on speed of reactions and the kinetic curves.in Heterogeneous reactions which the common surface area is not constant, but the reaction surface area has a certain geometric shapes such as sphere. The common surface area and reaction speed are changing gradually. According to the following equations, when passed reaction time, the common surface area and reaction speed is reduced:

[Equation10]:

dmdt=kAc

Where m(=43πr3ρ) is amount of core that is under reaction, r is radius of core and ρ is density  , A =4πr2  is common area, t is the time, k is chemical rate constant, c is concentration of chemical reagent.

[Equation 11]:           r=(3m4πρ)13

[Equation12]:          A =4π(34πρ)23 m 23

[Equation 13]:   -m0mdm=kAc0tdt

[Equation 14]:    kAc=k4π(34πρ)23 m 23c=k´m23

[Equation 15]:          3m023-m13=k´t

When one part of the mineral reacts, the speed of reaction properly states by the value of R. following equations for spherical samples considered:

[Equation 16]:

Ri=nini,initial

Where (ni) is the number of moles of reagents in the reaction, time (t) the starts from the n1 of mole until nii reagents.

[Equation 17]:              R=m0-mm0

[Equation 18]:                  R=43πr03ρ-43πrc3ρ43πr03ρ=1-rc3r03

[Equation 19]:  rc=r0(1-R)13

Where rc is the range of the reacted particle, r0 is the range of the unreacted particle [20, 21, 22].

The shrinking core model (SCM), describes solid particles are being consumed through dissolution reaction. Shrinking core is the amount of core that being consumed. In SCM, the dissolution depend on different parameters ; the material exchange in reaction  during the dissolution, the diffusion of products and reagents over the surface of the particles among of product layer in the core, and chemical reaction. The rate of reaction was consisted on, R, to equation (20), [23]:

[Equation 20]:

kct = 1- (1-R)1/3

Where t is the reaction time and kc is the rate constant for the reaction, assumed by [24,25].

[Equation 21]:

kc=     MbksCfs r0ρz

Where b is the stoichiometric coefficient, M is the molecular weight of the sulphide mineral, ks is the chemical rate constant, and cfs is the concentration of (Fe3+) in the sulphur layer on the surface, and ρz is the density of sulphide mineral. “Figure 5” is showed that there is a good fitting between chemical reaction control and SCM model, Crundwell confirmed that the leaching of sphalerite in the initial stages was controlled chemically and in the product layer controlled by diffusion layer [26]. These results are consistent with experimental data that, can be understood the kinetic of leaching controlled by reaction in the surface.

Figure 5:  Plot of 1-(1-R) ¹/³ with time, different temperature, particle size -75µm_+45µm, acid concentration of 5% (v/v) and manganese dioxide 20% (w/v) as oxidative agent.

The activation energy depends on the effect of temperature on (ks) follows the Arrhenius equation (22) and (23):

[Equation 22]:

ks=Ae-EaRT

[Equation 23]:

lnks=-EaR1T+lnA

Where Ea is the activation energy, A is the frequency factor, of the reaction, R is the universal gas constant, and T is the total temperature. The diffusion mechanism system has a characteristic Ea of 5 kcal (≈21 kJ/mol), and in this work, according to figure6 the activation energy determined by Ea=21.78 kJ/mol.

Figure 6: Plot of Arrhenius equation

due to existents several metals in this experiment in the sample but we need to extract one of them and may be part of the dissolution process spending metal or other impurities in the sample, in this part of reaction a unreacted layer is produced around the core, in these situations it can influence on the reaction speed through the reaction controlled by diffusion model “Figure7”. However there is a good fit between experimental data and diffusion model, the layer of elemental sulphur delays diffusion deceleration. The rate of reaction can be spoken by the Brounstein and Crank- Ginstling, model for diffusion over a non-porous produce layer [27]:

[Equation 24]:

kd t=1-23R-(1-R)2/3

Where kd is the rate constant for diffusion, assumed by:

[Equation 25]:

kd=     2MbDeCfs r02ρz

Where, (De) is the active diffusion coefficient of ions in porous medium.

Figure7:  plot of 1-23R-(1-R)2/3  with time, different temperature, particle size -75µm_+45µm, acid concentration of 5% (v/v) and manganese dioxide 20% (w/v) as oxidative agent.

Effect of different particle size

The influence of particle size on the recovery showed by “Figure 8” that with reducing in size of the particles, the zinc recovery increases.

Figure8: Effect of different particle size, Temperature 338 K acid concentration of 5% (v/v) and manganese dioxide 20% (w/v) as oxidative agent.

# CONCLUSION

In this work, the kinetics of the leaching of sphalerite concentrate were studied. The effects of the experimental parameters such as different particle size, the temperature, sulfuric acid and oxidative agents concentrations, were analyzed.

When the sulfuric acid concentrations increase, the rate of dissolution increases. Therefore, PH adjustment reactions play an important role in the development of zinc dissolution, so this parameter also is impressive by changing the amount of acid concentration. The optimum leaching conditions were determined to be: particle size +75µm_+45µm, acid concentration of 5% (v/v) and in presence of manganese dioxide 20% (w/v), it is clear that increasing temperature has a significant impact on the recovery. Especially in the temperature of    85 ° C maximum amount recovery was obtained. The kinetic data was analyzed by SCM model. The new SCM model fits the kinetic data appropriately. The activation energy was calculated by Ea=21.78 kJ/mol.

The main role of manganese dioxide or other oxidative agents is to re-oxidize the ferrous ions to the ferric ions. The usage of ammonium persulphate as oxidants, showed that the chemical processes of this reaction are similar to the previous mode reaction and the oxidative agents have impact on the re-oxidizing the ferrous ions to the ferric ions in, the ferric ions play as dissolution agent to solution zinc dissolution sphalerite during reactions. Results of two experiments indicated that; manganese dioxide shows better performance rather than ammonium persulphate during leaching.

# References

[1] Dutrizac, J.E.; Macdonald, J.C. The dissolution of sphalerite in ferric chloride solution. Metall. Trans. B 1978, 9B, 543–551.

[2] Habashi, F. The Metal Industry Ferrous Metals; WILEY-VCH:Weinheim, Germany, 1997; Volume I.

[3] F.K. Crundwell. ” The dissolution and leaching of minerals Mechanisms, myths and misunderstandings”, Hydrometallurgy 139 (2013) 132–148.

[4] SOUZA A D, PINA P S, LEÃO V A. Bioleaching and chemical leaching as an integrated process in the zinc industry [J]. Minerals Engineering, 2007, 20(6): 591−599.

[5] DELLER G. World zinc supply and demand-heading for a late decade price spike [C]//UMETSU Y. Lead & Zinc’05. Kyoto: The Mining and Materials Processing Institute of Japan, 2005: 17−25.

[6] Van PUT J W, TERWINGHE F M I G, de NYS T S A. Process for the extraction of zinc from sulphide concentrates: US 5858315 [P]. 1999−01−12.

[7] FUGLEBERG S, JÄRVINEN A. Method for leaching zinc concentrate in atmospheric conditions: European WO/1998/006879 1998−02−19.

[8] LI Ruo-gui. Atmospheric oxygen-rich direct leaching of zinc concentrate [J]. China Nonferrous Metallurgy, 2009(3): 12−15, 21.

[9] CHEN Yong-qiang, QIU Ding-fan, WANG Cheng-yan, YIN Fei. Oxygen-enriched leaching of zinc sulfide concentrate in atmospheric pressure equipment [J]. Nonferrous Metals, 2009, 61(4): 60−64.

[10] SVENS K, KERSTIEN B, RUNKEL M. Recent experiences with modern zinc processing technology [J]. Erzmetall, 2003, 56: 94−103.

[11] TAKALA H. Leaching of zinc concentrates at Outokumpu Kokkola Plant [J]. Erzmetall, 1999, 52: 37−42.

[12] HAAKANA T, SAXÉN B, LEHTINEN L, TAKALA H, LAHTINEN M, SEVENS K, RUONALA M, GONGMING X. OUTOTEC direct leaching application in China [J]. Journal of the South African Institute of Mining and Metallurgy, 2008, 108(5): 245−251.

[13] CHEN Yong-qiang, QIU Ding-fan, WANG Cheng-yan, YIN Fei. Oxygen-rich leaching of sphalerite concentrate under normal pressure [J]. The Chinese Journal of Process Engineering, 2009, 9(3): 441−448.

[14] Fabrício Eduardo Bortot Coelhoa et al,” Roasted zinc concentrate leaching: Population balance modeling and validation”, Hydrometallurgy 175 (2018) 208–217.

[15] Teresa Pecina, Telhma Franco, Pedro Castillo, Erasmo Orrantia.”  Leaching of a zinc concentrate in H2SO4 solutions containing H2O2 and complexing agents”, Minerals Engineering 21 (2008) 23–30.

[16] M.N.Babu et al,” Zinc recovery from sphalerite concentrate by direct oxidative leaching with ammonium, sodium and potassium persulphates“,Hydrometallurgy Volume 64, Issue 2, May 2002, Pages 119-129.

[17] Jan et al. Jan, R.J., Hepworth, M.T., Fox, V.G., A kinetic study on the pressure Leaching of sphalerite, Metallurgical Transactions B 7B (1976) 353-361.

[18] Jan, R.J., Hepworth, M.T., Fox, V.G., A kinetic study on the pressure leaching of sphalerite, Metallurgical Transactions B 7B (1976) 353-361.

[19] Verbaan and Crundwell Verbaan, B., Crundwell, F.K., An electrochemical model for the leaching of a sphalerite concentrate, Hydrometallurgy 16 (1986) 345-359.

[20] F.K. CRUNDWELL and B. VERBAAN.” Kinetics and Mechanisms of the Non-oxidative Dissolution of Sphalerite (Zinc Sulphide)”, Hydrometallurgy, 17 (1987) 369-384.

[21] Akcil, A., Ciftci, H., Metals recovery from multimetal sulphide concentrates (CuFeS2-PbS-ZnS): combination of thermal process and pressure leaching, Int. J. Miner. Process. 71 (2003) 233-246.

[22] Levenspiel, O., 1999. Chemical Reaction Engineering. John Wiley & Sons, New York. 664pp.

[23] Bobeck, G., Su, H., The kinetics of dissolution of sphalerite in ferric chloride solution, Metallurgical Transactions 16 B (1985) 413-424.4.

[24] Lochmann, J., Pedlik, M., Kinetic anomalities of dissolution of sphalerite in ferric sulfate solution, Hydrometallurgy 37 (1995) 89-96.10.

[25] Bobeck, G., Su, H., The kinetics of dissolution of sphalerite in ferric chloride solution, Metallurgical Transactions 16 B (1985) 413-424.4.

[26] F.K. CRUNDWELL and B. VERBAAN.” Kinetics and Mechanisms of the Non-oxidative Dissolution of Sphalerite (Zinc Sulphide)”, Hydrometallurgy, 17 (1987) 369-384.

[27] Ginstling A.M, Brounstein B.I., О,” Diffusion kinktics of reactions in spherical particles”, Journal of Applied Chemistry, 1950, 23(12), 1249-1259, (In Russian).